How to Melt Metal Material by Induction Heater

SP-15A and SP-16A  induction heaters can be used for melting  Pb, Cu, Ag, Au and ferrous metal.

In order melt metal material efficiently, you shall use graphic crucible and  refractory insulating layer. Sketch below shows typical crucible set-up.

Max heating temperature is about 1700oC , which depended on  sample quantity,  heated crucible size  and thickness of thermo insulating layer .  You shall test buy yourselves and find the best way for your application

Quartz liner if < 1200oC

Alumina liner if >1200oC

Induction Coil

Graphite crucible if < 1200oC

Platinum crucible if >1200oC

SP-15A (7Kw) or SP-16A (16KW)

Ferrous metal charger

Induction heater

Thermal couple, S  type

Temperature display

Porous Alumina ceramic support crucible

Cooling water

If you try to melt metal which is easy to oxide in air, you may consider to set up a crucible with vacuum flange as the follow:

Vacuum flange with valve

Ceramic plate on flange

Bottom close quartz tube

Quartz liner if < 1200oC

Alumina liner if >1200oC

Graphite crucible if <1200oC

Platinum crucible if >1200

Induction coil

How to build a Vacuum Induction Heater

55 mm

30 I.D

40 OD

65 mm I.D coil

Slide

Quartz jar

60 mm dia. X 2500mm Length

Thermo-couple