MTI Corporation

860 South 19th Street

Richmond, CA 94804

Tel: 510-525-3070   Fax: 510-525 4705

Website: www.mtixtl.com  Email: sales@mtixtl.com

Notes for all metallic substrates users:

Prior to the deposition process, please always clean surface to remove oxidation layer

Recommended clean procedure is as follow:

- Start vacuum to 10-4 torr

- Heat the metallic substrate above 700oC

- Fill the vacuum chamber with hydrogen gas to remove any oxidation layer

- Shut down the hydrogen gas and lower the temperature to the operation temperature.

MTI is not response for any damage and fail test caused by end user.